Acceptance Criteria & Limits (ACL) — CYG-21700-50G

Cygnus Cell Technologies  |  Document ACL-CYG21700-00  |  Framework IESF-4400

The following acceptance limits apply to qualification testing. Limits are organised by duty profile. Where a parameter row carries a marker, the corresponding note at the foot of this document applies.

Duty Profile: Automotive Traction   (conditioning rates: 0.5C, 1.0C)

| Sr. No. | Test Parameter | Acceptance Limit | IESF-4400 Clause |
| --- | --- | --- | --- |
| 1 | Capacity Verification | ≥ 98.0 % of rated capacity at 0.5C, 25 °C * $ | §6.2 |
| 2 | DC Internal Resistance (DCIR) | ≤ 18 mΩ at 50 % SOC, 25 °C # | §6.3 |
| 3 | Cycle-Life Endurance | ≥ 80 % capacity retention after 500 cycles $ | §6.4 |
| 4 | Overcharge Tolerance | No fire, no explosion at 1.5 × V_max charge @ $ | §6.7 |
| 5 | External Short-Circuit | Case temperature ≤ 80 °C; no fire @ | §6.9 |
| 6 | Thermal Stability (Hot-Box) | No fire, no explosion after 130 °C / 30 min soak @ | §6.11 |
| 7 | Altitude Simulation | No leakage; ≤ 1.0 % capacity loss at 11.6 kPa / 6 h | §6.12 |

Duty Profile: Grid Storage   (conditioning rates: 0.5C)

| Sr. No. | Test Parameter | Acceptance Limit | IESF-4400 Clause |
| --- | --- | --- | --- |
| 1 | Capacity Verification | ≥ 98.0 % of rated capacity at 0.5C, 25 °C (lot-acceptance) * $ | §6.2 |
| 2 | DC Internal Resistance (DCIR) | ≤ 18 mΩ at 50 % SOC, 25 °C # | §6.3 |
| 3 | Cycle-Life Endurance | ≥ 80 % capacity retention after 500 cycles $ | §6.4 |
| 4 | Overcharge Tolerance | No fire, no explosion at 1.5 × V_max charge @ $ | §6.7 |
| 5 | External Short-Circuit | Case temperature ≤ 80 °C; no fire @ | §6.9 |
| 6 | Thermal Stability (Hot-Box) | No fire, no explosion after 130 °C / 30 min soak @ | §6.11 |
| 7 | Altitude Simulation | No leakage; ≤ 1.0 % capacity loss at 11.6 kPa / 6 h | §6.12 |

Notes:

* Capacity limits apply to graded cells only; ungraded cells are assessed per IESF-4400 §6.2.1.

# DCIR is measured by a 10 s DC pulse at 1.0C and corrected to 50% SOC.

@ Mechanical-abuse limits apply to cylindrical and prismatic formats; pouch cells are governed by Annex P.

$ The test voltage window is defined by the cell vendor datasheet electrical ratings, not by this table.